Specification of BNL p-type stripixel detector:

7/13/2005

Footprint:		6.4 cm x 3.0 cm

Pitch: 			50 um

Implant width: 	5 um

Metal width:		6 um

Isolation:		p-spray (or p-spray + p-stop)

p-implants:		Boron

# of Guard rings: 	2

Guard ring width:	300 um inner, 50 um outer

Distance to edge:	1650 um

Number of strips:	512 x, 512 u (x 2 halves)

Active width:		2.58 cm

Width:			2.986 cm

Active Length: 	5.97 cm

Total length:		6.37 cm

Pads			Staggered, 2 rows

# metal processes	2