GLAST Conductive Glue Discussion

Gwelen Paliaga

SCIPP

3/9/00

# REQUIREMENTS

- Room temperature cure.  (?)

- Compliant (to avoid stress concentration at bond edges)

- Thixotropic (doesn’t flow)

- High Strength (to prevent ladder buckling and bond line peeling- recent results)

- Operating temperature  -55 C to 60 C

- Meets NASA outgassing specs

- Safe for semiconductors (low ion content)

# USE

- Mechanical and electrical connection of SSD to Kapton bias circuit.

- 4 mil bond line (can be adjusted, but affects tower geometry).

# ISSUES

- Silver migration

- Aging

- Room temperature cure with low outgassing

- Ion content

# CANIDATES

| Company | Name | NASA approved | Min. Cure Temp, (C) | Comments |
| --- | --- | --- | --- | --- |
| Nusil | CV-2640 | Yes | 25 | Silicone, carbon filled, resistivity icreased a lot with thermo-cycling |
| AI Technology | ME8456 | Yes | 80 | Compliant, benchmark material for NASA, Lockhead, Boeing |
| Epo-Tek | H20E | Yes | 50 |  |
| Epo-Tek | 8 other possibilities | YES | High |  |