HYBRID DESIGN/ASSEMBLY DEVELOPMENTS

THERMAL BONDING TO CLOSEOUT

SCIPP, 3/28/00

Gwelen Paliaga

MOTIVATION:

- Higher than expected temp. drop down tower wall

- Minimize temp. drop from HDI to thermal boss

- Use as mechanical bond  reduce # screws

- Provide seal for eventual wire-bond encapsulation

REQUIREMENTS:

- Room temp. cure (required for any bonding involving trays)

- Repairable – low peel strength

- Low outgassing

- Fast cure for manufacturability

- Thermally conductive > 0.3 W/mK

- Operating temp. range –55 to +60 C

Thermal Conductivity of Some Low Outgassing Adhesives

| Company | Type | Thermal Conductivity (W/mK) | Delta T (K) (for 2 mil bond line) | Percent of allowable 0.25 C drop |
| --- | --- | --- | --- | --- |
| Nusil | silicone | 0.84-1.5 | 0.0099-0.0053 | 2.1-4.0 |
| Epo-Tek | epoxy | 0.9-4.0 | 0.0092-0.0021 | 0.8-3.7 |
| Tra-Con | epoxy | 0.6-2.0 | 0.0138-0.0042 | 0.2-5.5 |
| 3M | tape | 0.43 | 0.0194 | 7.8 |

- Eric Ponslet agrees that 16% of 0.25 C drop over bond line is acceptable

POTENTIAL MATERIALS:

- 2-sided tape – 3 potential space qualified materials have been found

- silicones – many space qualified materials have been found

| Name | Company | Type | Thermal Conductivity (W/mK) | Peel Strength (N/m) | Cure Time | Cure Pressure (psi) |
| --- | --- | --- | --- | --- | --- | --- |
| CV-2943 | Nusil | Silicone | 1.26 | 16600 | 7 days | NA |
| CV-2902 | Nusil | Silicone | 0.84 | 14000 | 7 days | NA |
| 9882 | 3M | Transfer Tape | 0.43 | 40-80 | Short | moderate? |
| Thermattach T412 | Chomerics | Tape w/ backing | 1.4 | ? | 15 sec. | 10 |
| Thermattach T405 | Chomerics | Tape w/ backing | 0.5 | ? | 15 sec | 10 |

TAPE:

- Desirable due to ease of manufacturing and reparability

- Generally lower thermal conductivity (probably not an issue)

- More difficult to get thermal contact – requires high planarity

- Is aging an issue? “tape bonds get stronger over time” – Chomerics data sheet

- Would possibly motivate more screws

SILICONE:

- Flexible and repairable

- Extremely long cure time at room temp.  Set up time may be shorter?

OTHER OPTIONS:

- Fairly extensive search was done

- Custom formulate by adding filler ourselves – has been done and documented by NASA

- Find epoxy, or silicone with more desirable properties and add Al Nitride or Boron Nitride filler